Table of Contents

1.	PRE REQUISITES	2

2. APPARATUS AND EQUIPMENT REQUIRED	2

3. PROCEDURE (FURNACE METHOD)	2

3.1. Sample preparation	2

3.2. Analysis method	2

4. Calculation	3

5. Revision table	3

## PRE REQUISITES

note: Only personnel who are declared competent are to perform laboratory activities. personnel not declared are to strictly work under supervision of a lab manager/supervisor or competent personnel.

- Ensure that all wet coarse and fly ash samples are dried in an oven 105oC for 1 hour before testing.

- Ensure that coarse ash samples are ground down to be fine.

- Personnel must always wear a mask during sample handling.

## 2. APPARATUS AND EQUIPMENT REQUIRED

- Analytical balance

- ISO furnace

- Pestle and mortar

- Watch glass and spatula

- Heat resistant crucibles

- Pair of tongs with hand shield

## 3. PROCEDURE (FURNACE METHOD)

## 3.1. Sample preparation

- Upon receipt of the samples, transfer wet coarse ash into a tray and dry in an oven set to 105oC.

- After drying and cooling, mix thoroughly to obtain a representative sample.

- Grind the coarse ash using pestle and mortar until it is fine enough to pass through a 75µm mesh

## 3.2. Analysis method

- Weigh 1g of sample in duplicate into clean, dry crucible, and spread the material evenly on the surface of the crucible.

- Use a pair of tongs and carefully place the samples into the ISO Ash furnace.

- Press RUN button on the furnace controls to initiate the test cycle.

- Allow the ISO furnace to ramp and reach 815oC until END appears on the display panel.

- Cool for 10 minutes on the bench, and 10 minutes in the desiccator.

- Weigh the final mass of crucible+contents.

## 4. Calculation

#### %Carbon = (100- M3-M1M2-M1) X 100

## 5. Revision table

| Revision no | Content changed | Reason for revision | Date changed |
| --- | --- | --- | --- |