Contents

General Information	2

Materials, Equipment & Verification	3

Processing Plan and Workflow	5

Homogeneity and Stability Assessment	6

Measurement Procedures	6

Risk Assessment	6

Risk Management	7

Revision Table	7

This master document governs the design, statistical strategy, preparation, testing, and distribution of Proficiency Testing (PT) items for coal analysis. It applies to all PT testing items that fall under the scope of the laboratory.

## General Information

| Field | Entry |
| --- | --- |
| PT Scheme | September GA/HGI 09/2026 |
| Unique Batch Number | September GA/HGI 09/2026 |
| Intended Use | Proficiency Testing Sample & Competency Evaluation and monitoring of staff |
| Matrix Type | Pulverized Coal (< 212 µm) OR Prepared Coal Sized Material (4.75 mm) |
| Properties to be assigned | ISO Ash, ISO Volatile Matter, Calorific Value, Total Sulphur, Inherent Moisture OR Hardgrove Grindability Index (HGI) |
| Production Start Date | Start of PT round |
| Production End Date | End of PT round |
| Expected Participants | 10 – 30 Laboratories |
| Responsible Person | PT Scheme Coordinator |
| Approved By | Operations Manager |

## Materials, Equipment & Verification

A list of materials and equipment to be used in the production of the PT testing item are tabled and listed as follows:

General Analysis:

| Item | Description/Specs | Supplier | UoM | Verification Date | Verified By | Serial Number | Qualification Service |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Raw Material | Bituminous coal sample |  | - |  |  | - | Approved |
| Crushers | 25,10,3 (mm) | MegaSize | - |  |  | 202203331 SC, AS8809, A124119; respectively | Cleaned and verified |
| Pulverizer | 212 μm | MegaSize | - |  |  | 22L90713190645 | Cleaned and verified |
| Platform Scale | 0.01 Kg | Darvan Brenco | ±0.03 kg |  |  | 120330150 | Calibrated |
| IM Moisture Oven 50L | Maintain a temperature of 107oC | Darvan Brenco | ±1.0 oC |  |  | DOV53A/210325/40 | Calibrated |
| Mass pieces | 1 to 100 (g) | Micron | ±0.00014 | April 2025 | Micron | OB WS1.1R | Calibrated |
| Ash Furnace | Maintain 815±10oC for at least 1 hour | Micron (ATS) | ±4 oC |  |  | ATS/210325/7A | Calibrated |
| ISO Volatile Matter Furnace | 900oC±5oC | Micron (ATS) | ±3 oC |  |  | ATS/210325/59V | Calibrated |
| Analytical Balance | 0.0010g | Micron | 0.0003g |  |  | ITA2500477, AS2156 | Calibrated |
| Top Balance | 0.1g | Micron | 0.3g |  |  | AEA90242156, AS00A31 | Calibrated |
| Packaging Material | ±150 g | Foamy | - | - | - | - | Cleaned |
| Homogeneity Drum | - | - | - | Checked upon homogeneity test | - | - | Cleaned |

Hardgrove Grindability Index:

| Item | Description/Specs | Supplier | UoM | Verification Date | Verified By | Serial Number | Qualification Service |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Raw Material | Bituminous coal sample | Lungiles Pyrite | - |  |  | - | Approved |
| Crushers | 25mm, 10mm & 4.75mm | MegaSize | - |  |  | 202203331 SC, AS8809, & A124119 | Cleaned and verified |
| Test Sieves | 1mm, 3mm & 4.75mm | Micron | - | Sept 2024 Jan 2025 |  | 500401, 500623 & 500628 | Verified |
| Platform Scale | 0.01 Kg | Darvan Brenco | ±0.03 kg |  |  | 120330150 | Calibrated |
| Drying oven | Maintain a temperature of 40oC | MegaSize | ± 1.0°C |  |  | LZ 007/07/10 | Calibrated |
| Mass pieces | 1 to 100 (g) | Micron | ±0.00014 | April 2025 | Micron | OB WS1.1R | Calibrated |
| Ash Furnace | Maintain 815±10oC for at least 1 hour | Micron (ATS) | ±4 oC |  |  | ATS/210325/7A | Calibrated |
| Analytical Balance | 0.0010g | Micron | 0.0003g |  |  | ITA2500477, AS2156 | Calibrated |
| Top Balance | 0.1g | Micron | 0.3g |  |  | AEA90242156, AS00A31 | Calibrated |
| Packaging Material | ±150 g | Foamy | - | - | - | - | Cleaned |
| Homogeneity Drum | - | - | - | Checked upon homogeneity test | - | - | Cleaned |

NB: The supplier of the materials will vary due to the required CRM quality to be produced. However, it is required that a record of list of suppliers of coal associated which a specific CRM be maintained at the laboratory. This is to ensure that the same CRM will be produced that is consistent with the initial quality produced.

NB: All other equipment used for the preparation and testing; the validation or equipment maintenance are specified in the respective coal testing methods ie. Procedure on sample preparation of Hard coal has detailed how to use crushers and efficiency requirements needed to produce coal size material required.

## Processing Plan and Workflow

General Analysis

| Step | Description | Equipment used | Environmental Conditions | Acceptance criteria |
| --- | --- | --- | --- | --- |
| 1 | Air drying | - | Atmospheric temperature | The sample should be visibly dry |
| 2 | Stage Crushing | 25,10,3 mm Crushers | Room temperature | Crusher Efficiency ≥90% |
| 3 | Pulverizer | Serial no: 22L90713190645 | Room temperature | Pulverizer efficiency ≥95% |
| 4 | Homogeneity Drum | - | - | ¬ 4 hours |
| 5 | Homogeneity Validation (analysis) | Ashing Furnace & Inherent moisture Oven | 19-26oC | ANOVA, SSbetween<Check Value |
| 6 | Packaging | ±150g | Room temperature | - |
| 7 | Storage | Storage room | ≤ 20oC | Temperature <23oC |

Hardgrove Grindability Index

| Step | Description | Equipment used | Environmental Conditions | Acceptance criteria |
| --- | --- | --- | --- | --- |
| 1 | Air drying | - | Atmospheric temperature | The sample should be visibly dry |
| 2 | Stage Crushing | 25,10,3 mm Crushers | Room temperature | Crusher Efficiency ≥90% |
| 3 | Screening | Serial no: 22L90713190645 | Room temperature | Pulverizer efficiency ≥95% |
| 4 | Homogeneity Drum | - | - | ¬ 4 hours |
| 5 | Homogeneity Validation (analysis) | Ashing Furnace Inherent moisture Oven | 19-26 °C | ANOVA, SSbetween<Check Value |
| 6 | Packaging | ±150g | Room temperature | - |
| 7 | Storage | Storage room | ≤ 20°C | Temperature <23°C |

## Homogeneity and Stability Assessment

| Assessment Type | Method | No of units | Statistics By | Parameter | Acceptance Criteria |
| --- | --- | --- | --- | --- | --- |
| Homogeneity | ASIW001 | 10 | PT Scheme Coordinator | Q-Ash and IM | ANOVA, SSbetween<Check Value |
| Stability | ASIW001 | 10 | PT Scheme Coordinator | Q-Ash and IM | Reproducibility between homogeneity & stability means < homogeneity check value |

## Measurement Procedures

| Parameter | Method Reference | Equipment | Analyst |
| --- | --- | --- | --- |
| Q-Ash | ISO 1171 | Furnace | Laboratory Analyst |
| Volatile Matter | ISO 562 | Furnace | Laboratory Analyst |
| Calorific Value | ISO 1928 | Bomb Calorimeter | Laboratory Analyst |
| Inherent Moisture | SANS 5925 | Drying Oven | Laboratory Analyst |

NB: The following authorised procedures are to be used:

- AS002IW Procedure on the conditioning of samples,

- AS003IW Procedure for the determination of Ash content

- AS006IW Procedure for the determination of Volatile Matter

- AS004IW Procedure on the determination of Inherent Moisture

- AS007IW Procedure on the Calorific Value determination.

## Risk Assessment

| Risk Description | Impact | Mitigation strategy |
| --- | --- | --- |
| Power outage during analysis | Low | Backup generator |
| Balance drift | Medium | Verification with calibrated mass pieces at the beginning of every shift. |
| Sample Swap | High | Prepare one sample at a time, only after packaging has been completed then the next sample can be prepared. |

# Risk Management

| Record Type | File Name/ Location | Responsible Person | Retention Period |
| --- | --- | --- | --- |
| Batch Processing | Form | Laboratory Supervisor | 5 years |
| Analytical Results Sheet | LIMS | Laboratory Supervisor | 5 years |
| Homogeneity Test report and Stability Test report | Final PT report or website | PT Scheme Coordinator | 10 years |
| Calibration Certificates | Technical File | Lab Manager | 5 Years |

# Revision Table

| Contents Changed | Reason for Change | Revision | By whom | Date |
| --- | --- | --- | --- | --- |
| Addition of HGI production planning | Incomplete system documentation | Revision 01 | Keitumetse Maleka | 06/10/2026 |