SAMPLE PREP FLOW DIAGRAM

AIR DRY THE SAMPLE UNTIL VISIBLY DRY

STAGE CRUSH THE SAMPLE (-25MM AND THEN -10MM)

SPLIT THE SAMPLE

TM

GA

HGI

CRUSH IN THE -3MM

HOMOGENEOUS THE SAMPLE IN MIXER FOR 1 HOUR

HOMOGENEOUS SAMPLE IN THE MIXER FOR 1 HOUR

AIR DRY IN OVEN NOT EXCEEDING 40OC

SCREEN THE SAMPLE USING 0.5 MM

PULVERISE ENTIRE SAMPLE

CRUSH IN -3MM

CRUSH IN -3MM

HOMOGENEOUS THE SAMPLE IN MIXER FOR 4 HOURS

TAKE RANDOM GA SAMPLES FOR VALIDATION

(10-15)

WEIGH ± 2KG AND TRANSFER INTO PACKAGING CONTAINER

EXTRACT 600 G PORTIONS USING FLAT HEAP METHOD

WEIGH ± 2KG AND TRANSFER INTO PACKAGING CONTAINER