# PERSONNEL

Candidate name: 			 Position (Technical Signatory): 		 Assessment Date:

# Technical Knowledge and Theory

  - The candidate must demonstrate a thorough understanding of the following principles:

  - Standard compliance: Understand the requirements of ISO 1953 for coal sieving.

  - Sample Integrity: Knowledge of the minimum mass requirement (65kg) for statistical representation of top-size particles.

  - Fraction Management: Rationale for “scalping” at 22.4 mm to protect delicate fine mesh sieves

  - Calculation: Fractional Percentage = (𝑀𝑎𝑠𝑠 𝑟𝑒𝑡𝑎𝑖𝑛𝑒𝑑) 𝑋 100

𝑇𝑜𝑡𝑎𝑙 𝑚𝑎𝑠𝑠

# Practical Competency Checklist

| Task Item | Competency requirement | Outcome (P/F) |
| --- | --- | --- |
| Sample Prep | Correct use of “cone and quarter” method to extract representative sample. |  |
| Drying | Ensure the coal is visibly dry |  |
| Scalping | Proper separation of coarse material and fine fractions |  |
| Coarse analysis | Execution of the 360 oC revolutions, 8 back-and-forth agitations per segment. |  |
| Loading limits | Sample must cover at least ¾ of the total surface area, this to prevent particle breakage and/or restricted movement. |  |
| Fine analysis | Use lids/plastics for dust control and observing the 45-60s settling time. |  |
| Sieving Time | Precise timing of 2 minutes for the fine fraction analysis. |  |

# Data Validation & Quality control

A TS must be able to validate results based on the following criteria:

Mass loss correction: Any difference between the dried initial mass and the sum of recovered fractions must be added back to the “fines” mass (add to the smallest screen).

Recovery limits: Total recovery must lie 99.9≤R≤100.01 (%) to be considered valid.

Corrective action: Identify that dust loss is the most likely source of error if mass balance fails.

Precision: Ensure that major fractions remain within the ~2% absolute repeatability limit as specified by ISO 1953.

# Results

| Sample ID: |  |
| --- | --- |
| Analysis Date: |  |
| Personnel: |  |
| Initial mass dried (kg): |  |

| Sieve size (mm) | Mass retained (kg) | % Retained |
| --- | --- | --- |
| +50mm |  |  |
| +45mm |  |  |
| +40mm |  |  |
| +31.5mm |  |  |
| +25mm |  |  |
| +22.4mm |  |  |
| +12.5mm |  |  |
| +6.3mm |  |  |
| +3mm |  |  |
| +1mm |  |  |
| -1mm (+mass loss correction due to dust loss) |  |  |
| Total Recovered |  |  |

# NB: Empty spaces can be used for other screen sizes

Pass or Fail? :

# Authorisation

Employee signature:

# AUTHORIZING OFFICER

Name: 		 Designation:		 Date: 	 Authorizing Signature

Declaration: I hereby certify that the candidate has demonstrated the technical proficiency required to review, interpret, and sign off on the test results for PSD under AS014IW.