# INDEX

# Contents	             Page

- SCOPE...........................................................................................................................	2

- RESPONSIBILITIES AND AUTHORITIES ................................................................	2

- WORKING INSTRUCTION ........................................................................................	2

4         TABLE OF REVISION ...........................................................................................................	3

- SCOPE

The preparation area and analysis area have different environmental conditions, and as such, the sample must be conditioned before any analysis can be conducted. Conditioning allows the sample to be at equilibrium with the analysis room (humidity and temperature). This ensures that the sample is in the best possible state of use, which improves the reliability and accuracy of results.

- RESPONSIBILITIES AND AUTHORITIES

  - Shift Supervisor

  - Analyst

  - Laboratory Manager

- WORKING INSTRUCTION

- After the sample has been reduced to -212 µm (pulverized) and transferred into a clean 60-100g bottle, it shall be sent into the analysis room.

- The analyst shall transfer the sample into a clean tray and evenly spread it across the face of the tray.

- The bottle and lid should also be next to the tray, to allow the identification of said sample.

- Log the sample in the sample conditioning form (AS018TF)

- A sample will be left for at least 45min and not more than an hour in a stable environment (temperature should be maintained at 19oC – 26oC and RH at 25% to 60% as per AS specs)

- Transfer the sample back into the original container and close it.

- Record the bottling time on the sample condition form (AS018TF)

- Ensure that all the fields on the (AS018TF) are filled, this includes the name of analyst, signature and date.

| Table of Revision |  |  |
| --- | --- | --- |
| Rev number | Date | Reason for revision |